## Slide 1
PWO Crystal Production and Quality Control at SIC
Dr. Hui YUAN
SIC and JLab. Collaboration meeting, Shanghai, 2018.07.23

## Slide 2
Modified Bridgman method
PWO crystals production
PWO quality control
Summary
Outline

## Slide 3
Czochralski
Bridgman
Crystal Growth
High quality
High cost
High temperature
High efficiency
Low cost
High flexibility

## Slide 4
Speed：0.4-0.6 mm/h
Gradient：20-50 C/cm
Furnace temp：1170 C
Seeding temp: 1045 C
Furnace temperature profile
PWO Crystal Growth Parameters
Modified Bridgman Method

## Slide 5
Profile of modified multi-crucibles Bridgman furnace
Modified Bridgman Method

## Slide 6
2001.5-2002.6, SICCAS provided PrimEx all 1275 PWOs.
PWO CX for PrimEx

## Slide 7
PWO CX for PrimEx

## Slide 8
PWO CX for CMS
2005.6-2008.3, SICCAS provided CMS more than 5000 PWO crystals, totally about 7.6 tons.

## Slide 9
Process flow diagram
Recycle
Weighting
Polycrystalline
Shaping
Seeding
Crystal Growth
Ingots
Annealing
Machining
Test Bench
Products
Crucibles
Refining
Pt Fragments
Leak Checking
PWO Production

## Slide 10
Weighting
PbO/WO3 + 150ppm Y
Polycrystalline
Mixture sintered/melted
Shaping
Compounds into crucibles with seeds
Seeding
      Crucibles into furnace and heated
      Crystal growth
      Seeding temp reach and growth starts
PWO Production
Production procedures:

## Slide 11
Ingots
After finish, ingots got from crucibles
7. Annealing
Low temp annealing to remove tension
8. Machining
Cutting, grounding and polishing
Test bench
Transmittance, light yield and RH
      10. Products
      About 8 weeks needed
PWO Production
Production procedures:

## Slide 12
Lead time: 3-6 months
Furnace tuning, raw material ordering, Pt rental
PbO material
Environmental policy restrict the PbO production
Uniformity
      30 cx in one growth, no forced convention
      4. Crystal yield
      Growth * machining * performance
PWO Production
Key points:

## Slide 13
PbO material
For each batch, to grow one sample to verify the quality. Second source may be needed.
2. Uniformity
New furnaces are planned to be set up.
3. Radiation hardness
Gamma-ray irrad facility has been moved. UV irrad will be applied to the ingots to verify its RH.
PWO Quality Control

## Slide 14
PbO material
For each batch, to grow one sample to verify the quality. Second source may be needed.
2. Uniformity
New furnaces are planned to be set up.
3. Radiation hardness
Gamma-ray irrad facility has been moved. UV irrad will be applied to the ingots to verify its RH.
PWO Quality Control

## Slide 15
1. The PWO crystals can be produced with the Bridgeman technique.
2. Due to the environmental policy, PbO material supply is being reduced, and there is no nearby Gamma ray irrad facility.
3. New furnaces are planning to be set up.
Summary

## Slide 16
Thanks!